## Slide 1
Energy Storage from
Pseudocapacitive Materials
Bruce Dunn
Department of Materials Science and Engineering
UCLA

## Slide 2
Fundamentally different electrodes
  Batteries – redox reactions Supercapacitors – double layer
  Leads to different charge storage mechanisms and applications
Supercapacitors
Batteries
Energy Storage Technology Comparison

## Slide 3: Background: Energy vs. Power
Energy – the capacity to do work Power – how fast the energy is delivered
sub-second time response
P. Simon, Y. Gogotsi.. Nature Materials 7 (2008) 845-854
We are beginning to blur the distinction between batteries and capacitors

## Slide 4
Is there a need for materials/devices with
high energy and high power densities?
http://www.technologyreview.com/news/516876/
Tesla Aims to Charge
Electric Cars in Five Minutes
And the need is greater
for consumer electronics!

## Slide 5
Capacitive Charge Storage Mechanisms
Appeal of Pseudocapacitors: higher energy density than EDLCs
- Maintain same cycle life (1 M), short charging time (< 1 min)
- Achieve same power levels (10x of batteries)

## Slide 6: Cyclic Voltammetry and Experimental Set-Up for Electrochemical Measurements
Sweep rate controls the time scale of the experiment
Sweep the voltage and record current
Determine the limiting kinetics of the material
  Diffusion-limited
  Surface-limited
Potential (V)
Potential (V vs. Ag/AgCl)
Current (μA)
Time (s)
-10 -5 0 5 10
t0 t1 t2
0.1 0.3 0.5 0.7 0.9 1.0 1.1
Cycle 1
Cycle 2
Applied Stimulus
Output Response
Reference and Counter Electrode: Na Metal
Working Electrode: transition metal oxide particles suspended onto stainless steel foil
Electrolyte: 1M NaClO4in propylene carbonate

## Slide 7
Mechanisms of charge storage
Redox reactions
Lukatskaya, Dunn, Gogotsi; Nature Comm. (2016)

## Slide 8: Voltammetric Sweeps: Distinguishing between Batteries and Capacitors
A.G. Dylla, et al.,,
Acc. Chem. Res.
46 (2013) 1104.
Voltage
Voltage
dC/dV
dC/dV

## Slide 9
Signatures of Pseudocapacitive Materials
Capacitor-like kinetics
Peak current behavior
i(V) ~ avb i – current
V – potential v – sweep rate (mV/s)
b = 0.5; diffusion controlled behavior
b = 1.0; capacitor-like kinetics
Linear dQ/dV
Box-like CV

## Slide 10
Log sweep rate
Small voltage offset between redox peaks
No phase change on lithiation
Signatures of Pseudocapacitive Materials

## Slide 11
Intrinsic
Pseudocapacitors
Extrinsic
Pseudocapacitors
- Exhibit characteristics of pseudocapacitive
process:
- linear dQ/dV
- small redox DV
- not diffusion controlled
- No phase transformation on lithiation
- Nanoscale versions of bulk materials that
exhibit plateaus and phase transitions
- Exhibit some characteristics of pseudocapacitance: Linear dQ/dV, small DV between redox peaks; box-like CV
- Obtain by:
suppressing phase transitions (nanoscale materials), 2D layered materials (exfoliation), mesoporous materials.
High Rate Redox Materials

## Slide 12
Routes to Creating High Rate Energy Storage
1. Mesoporous materials
SEM image of mesoporous TiO2 film
after heating to 600oC.
Mesoporous architectures enable electrolyte access to redox-active walls
Interconnected porosity to ensure continuous electrolyte pathway and provide ionic conduction.
Nanodimensional walls (10 nm) beneficial for pseudocapacitive response.
Extending mesoporous systems to transition metal sulfides

## Slide 13
2. Exfoliated 2D sheets
Exfoliation of TiO2 with TBAOH
Peaks shift to lower energy
Peak Current
Peak Separation
55% capacitive
V. Augustyn et. al. Materials Horizons, 1, 219-223 (2014)
Routes to Creating High Rate Energy Storage

## Slide 14
Phase change with Li+ intercalation
(Monoclinic  Orthorhombic)
Li ion insertion (1electron)
(MoO2 + Li+ + e-  LiMoO2
Theoretical capacity
 753 C/g (210 mAh/g)
Phase change
Monoclinic Orthorhombic
(11% volume expansion)
Conversion reaction (3 electrons)
LiMoO2 + 3Li++3e-  Mo + 4Li2O
(628 mAh/g)
3. Nanomaterials suppressing phase transitions – MoO2
Routes to Creating High Rate Energy Storage

## Slide 15
Nanosized MoO2 does not show the phase transition
Hydrothermal synthesis leading to 15 – 20 nm diameter monoclinic MoO2 ; micron-sized materials purchased commercially
H. Kim et. al., J. Electrochem. Soc. 162, A 5083 (2015)

## Slide 16
MoO2 – Graphene Oxide Hybrid
Sweep Voltammetry:
Far better kinetic
response; MoO2 NPs on
conductive scaffold.
Hybrid exceeds nano
MoO2; charge to 75% of
theoretical capacity of
MoO2 in 30 seconds
Capacitive current
(b = 1) is over 80%
Galvanostatic Measurements:
Rate capability for hybrid is much
Better than nano-MoO2 ;
especially at high rates
Achieve 150 mAh/g at 50C
(Swagelok cell)
H. Kim et. al., J. Electrochem. Soc. (2015)

## Slide 17
▪ Hydrothermal microwave synthesis
- 270 mg MoCl5, 0.25 ml HNO3(70%), 5 ml EtOH, 15 ml DI water
- 170 °C, 15min, 200W
500 nm
Sample | (020) d (Å) | (040) d (Å) | (060) d (Å)
Reduced MoO3 | 7.031 | 3.505 | 2.335
Fully Oxidized MoO3 | 6.943 | 3.462 | 2.307
▪ Retain orthorhombic phase α-MoO3
▪ Deep blue color  reduced α-MoO3-x
X-value from TGA: MoO2.87
▪ Preferentially oriented to [010] direction
▪ 100 ~ 500 nm width and 1 ~ 5 μm length
Expand b-plane interlayers (wider vdW)
Routes to Creating High Rate Energy Storage
4. Oxygen deficient transition metal oxides – MoO3-x
Notes: Microwave synthesis
Hydrothermal: crystallizing substances from high-temperature aqueous solutions at high vapor pressures  slow crystallization kinetic
Microwave hydrothermal: The main advantage of microwave introduction into the reaction system is extremely rapid kinetics for synthesis.
Thickness of the MoO3 nanobelts ~ 10 nm (measured by AFM)

## Slide 18
Oxygen deficient MoO3 leads to better kinetics and improved
energy storage compared to oxidized
MoO3
Kim et. al. Nature Mater (2017)
Galvanostatic cycling at 30C
Swagelok cells, 2 mg/cm2 loading;
Electrode 80% MoO3-x/15 KB/5 PVDF
Performance at 10,000 cycles:
70% capacity retention to 90 mAh/g
99+% Coulombic efficiency
4. Oxygen deficient transition metal oxides – MoO3-x

## Slide 19
Thermodynamically stable phase is 2H form; trigonal prismatic coordination of S around Mo
On lithiation, first order phase change: 2H- MoS2 transforms to metallic 1T phase; Mo in octahedral coordination
6.2 Å
Other Routes to Creating Extrinsic Pseudocapacitance
High energy
density at high rates of charging and discharging
J.B. Cook, et. al. Adv. Energy
Materials (2016) 6, 1501937
5. Manipulating phase transitions- MoS2

## Slide 20
In total:
5 Components
4 Interfaces
2 Charge Transfers
Many sources of resistance
  Ionic
  Electric
  Charge Transfer
Materials are not devices: they are part of the device

## Slide 21
The case for energy storage:
Sol-gel chemistry has made significant contributions to
electrochemical storage
Current technology: Powder fabrication; coatings,
large scale synthesis
Unique features: orientation, pseudocapacitance,
tailored pore-solid architectures, encapsulated liquids
Future opportunities are certain to develop:
- architecture control (3D)
- integration with other constituents (graphene, CNT)
- multicomponent, nanoscale systems
Enabling alternate energy - Management of the grid
Lower CO2 emissions - Less dependence on imports
Chu and Majumdar,
Nature (2012) 488, 294
Energy Storage from Pseudocapacitive Materials

## Slide 22
Pseudocapacitive materials offer an opportunity to achieve high energy and high power density; materials moving towards the ‘white space’
Metrics identified to distinguish between batteries and capacitors
- redox reactions with b = 1 and small voltage offset
- no phase change on lithiation
dQ/dV is (almost) straight
reaching 100 mAh/g at 100C
Tailored morphology and modified chemistry lead to extrinsic routes for creating high rate energy storage and routes for cathode materials
High performance materials are becoming available, but we know very little about interfaces. Nonetheless, we can start to think about the design of prototype devices.
Energy Storage from Pseudocapacitive Materials

## Slide 23
Acknowledgements
Veronica Augustyn
Torsten Brezesinski
Jeremy Come
John Cook
Henri Gerard
Hyung-Seok Kim
Jason Kim
Jesse Ko
Chun-Han Lai
Terri Lin
Julien Polleux
Iris Rauda
Yan Yan
Laurent Pilon (UCLA)
Sarah Tolbert (UCLA)
Vidvuds Ozolins (UCLA)
Yunfeng Lu (UCLA)
Jeff Long (NRL)
Debra Rolison (NRL)
Patrice Simon (Toulouse)
Research Support:

## Slide 24
Thank you

## Slide 26
Three basic polymorphs: Orthorhombic (α-MoO3), Monoclinic and Hexagonal
Intercalation within the vdW gap as well as insertion in the Mo-O octahedron intralayer
Can accommodate up to 1.5 Li/Mo which is equivalent to 280 mAh/g
Large open channels in the layered structure provide fast Li-ion diffusion
Modest kinetics; irreversible phase transition (1st cycle) leads to poor cycling
Li, W.Y., Cheng, F.Y., Tao, Z.L., & Chen, J., J. Phys. Chem. B 2006, 110, 119 - 124
Schematic of [MoO6] octahedra in MoO3 units
Background on MoO3
Other Routes to Creating High Rate Energy Storage
2. Oxygen deficient transition metal oxides – MoO3-x
Notes: 26

## Slide 27
Synthesis and Characterization of Reduced MoO3
▪ Hydrothermal microwave synthesis
- 270 mg MoCl5, 0.25 ml HNO3(70%), 5 ml EtOH, 15 ml DI water
- 170 °C, 15min, 200W
500 nm
Sample | (020) d (Å) | (040) d (Å) | (060) d (Å)
Reduced MoO3 | 7.031 | 3.505 | 2.335
Fully Oxidized MoO3 | 6.943 | 3.462 | 2.307
▪ Retain orthorhombic phase α-MoO3
▪ Deep blue color  reduced α-MoO3-x
X-value from TGA: MoO2.87
▪ Preferentially oriented to [010] direction
▪ 100 ~ 500 nm width and 1 ~ 5 μm length
Expand b-plane interlayers (wider vdW)
Notes: Microwave synthesis
Hydrothermal: crystallizing substances from high-temperature aqueous solutions at high vapor pressures  slow crystallization kinetic
Microwave hydrothermal: The main advantage of microwave introduction into the reaction system is extremely rapid kinetics for synthesis.
Thickness of the MoO3 nanobelts ~ 10 nm (measured by AFM)

## Slide 28
Electrochemical Behavior and Phase Transitions
Ex-Situ XRD:
MoO3: Lithiation drives electrochemically induced phase transition
MoO3-x:
No phase transition; peaks indexed to (020) and
higher order; reversible Li+ insertion/extraction

## Slide 29
Higher capacity with reduced MoO3-x: formation of Mo4+
Ex-situ XPS with cycling (after 10 cycles at 10 mV/s)
Formation of Mo4+ oxidation state during cycling leads to high capacity
Mo4+ oxidation state is not observed at 3.5 V
Limited amount of Mo4+ obtained for MoO3
Reversible cycling behavior for MoO3-x
MoO3-x
MoO3

## Slide 30
Extended Cycling of Reduced MoO3-x
Galvanostatic cycling at 30C
Swagelok cells, 2 mg/cm2 loading;
Electrode 80% MoO3-x/15 KB/5 PVDF
Performance at 10,000 cycles:
70% capacity retention to 90 mAh/g
99+% Coulombic efficiency
On cycling:
redox peaks
diminish and
smaller voltage
offset
Kim et. al. Nature Mater (2017)

## Slide 31
Sheet of transition metal atoms between two similar sheets of chalcogen atoms.
Thermodynamically stable phase is 2H form; trigonal prismatic coordination of S around Mo
Strong internal bonds with weak bonds along c-axis between two slabs (vdW interaction).
vdW gap larger for nano MoS2: 6.9Å
On lithiation, first order phase change: 2H- MoS2 transforms to metallic 1T phase; Mo in octahedral coordination
Background on MoS2
6.2 Å
2H

## Slide 32
EtOH
PEO-bPBO
MoCl5
Stir 2 hrs
Humidity 4%
Add
1. Synthesis of mesoporous MoO2
Dip-coated on Pt coated Si; calcined at 350oC in 5% H2/95% N2
Synthesis of Mesoporous MoS2
2. Thermal sulfurization to MoS2
500°C/3 hr
5% H2S/95% Ar
MoO2 has 8 nm pores with 10 nm walls
After conversion to MoS2, pore size decreases to 5 nm
Lower density of MoS2 (5.1 vs. 6.5 g/cm3) causes decrease in pore size and thicker pore walls
Preferential orientation with
(002) in plane of substrate;
Pores enable electrolyte access
to (002) planes

## Slide 33
Conversion to 1T – MoS2
Peak at 1.1V in 2H phase become progressively smaller
Selected area diffraction shows that after 50 cycles pristine and cycled films correspond to different phases
167 mAh/g at x = 1
Rct decreases with cycling;
Initial increase is from SEI formation
Stephenson, et. al. Energy,
Environ. Sci. (2014) 7, 209

## Slide 34
Electrochemical Properties of MoS2 (1T)
Trasatti Analysis
q(v) = q∞ + constant(1/v1/2)
q(v): capacity (sweep-rate)
q∞: infinite sweep rate
k1 fraction
~ 90%
Total current from
voltammetry
Galvanostatic Expts

## Slide 35
Li4Ti5O12 data: N.Q. Zhang, et al.,
Electrochem. Commun. 13 (2011) 654.
10C-rate
C = dQ/dE
1 minute
Comparing Nb2O5 to other Composite Electrodes
MoO2

## Slide 36
Electrochemical characterization
■ Testing Setup
 Higher current response and higher capacity (800 C/g at 10 mV/s)
Stainless steel foil substrate
40 μg MoO3 from ethanol solution, dispersed onto 1 cm2
Lithium reference & counter electrodes
Working electrode
Electrolyte - 1M LiClO4 in PC
▪ Working electrode
▪ Electrochemical Cell
■ Cyclic voltammetry & rate capability
 Good cyclability (96 % initial capacity was maintained after 50 cycles)